Conventional Specification –Pressurized

| Heat pipe insert into manifold and contact with water indirectly. Liquid can be tap water or antifreeze. Model | Heat pipe Vacuum Tube |  |  | Manifold |  | Frame material | Pressure Resistance (Mpa) | Absorptive Area (㎡) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | NO. (pcs) | Outer Dia. (mm) | Len. (mm) | Material | Outer covering |  |  |  |
| SC58/10 | 10 | φ58 | 1700 | Copper | Aluminum Alloy | Aluminum Alloy | 0.7 | 0.77 |
| SC58/20 | 20 | φ58 | 1700 | Copper | Aluminum Alloy | Aluminum Alloy | 0.7 | 1.54 |
| SC58/30 | 30 | φ58 | 1700 | Copper | Aluminum Alloy | Aluminum Alloy | 0.7 | 2.31 |

Using slides to connect each part of frame and adjust location by yourself.

| Model | Heat pipe Vacuum Tube |  |  | Manifold |  | Frame material | Pressure Resistance (Mpa) | Absorptive Area (㎡) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | NO. (pcs) | Outer Dia. (mm) | Len. (mm) | Material | Outer covering |  |  |  |
| SQ58/10 | 10 | φ58 | 1700 | 304 Stainless steel | Aluminum Alloy | Aluminum Alloy | 0.7 | 0.77 |
| SQ58/20 | 20 | φ58 | 1700 | 304 Stainless steel | Aluminum Alloy | Aluminum Alloy | 0.7 | 1.54 |
| SQ58/30 | 30 | φ58 | 1700 | 304 Stainless steel | Aluminum Alloy | Aluminum Alloy | 0.7 | 2.31 |

Heat pipe insert into manifold and contact with water or liquid directly. Efficiency is better.

Heat Pipe Performance Parameter

| Degree of Vacuum | ≧5×10-3 Pa |
| --- | --- |
| Material of tube | High Boron Silicon Glass |
| Size of Condenser Header (mm) | φ16×70 |
| Coating | AL/AL-ALN；Cu/Ss-ALN |
| Absorptivity | ≧0.86% |
| Emissivity | ≦0.08% |
| Highest Temperature Under Sunshine | 250℃ |
| Wind Resistance | 30 m/s |
| Startup Temperature | ≦25℃ |
| Hailstone Resistance (mm) | 30 |
| Weight of single tube (Kg) | 2.4 |
| Size of single tube (mm) | φ58×1700 |
| Life | ＞10 years |